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DESCRIPTION
YHFloorSeal PW is a two-component aliphatic polyurethane coating formulated to a transparent matte finish. After full curing, it delivers superior mechanical performance with outstanding abrasion and scratch resistance. It also minimizes dirt accumulation, greatly simplifying routine cleaning and maintenance.
Formulated as an aqueous dispersion, the product is nearly odorless, perfectly suited for enclosed indoor areas and offering excellent workability for flooring contractors.
WHERE TO USE
YHFloorSeal PW is an ideal topcoat for resin flooring systems. The product is also suitable for the surface protection of concrete substrates. 
CHARACTERISTICS AND PACKAGING
	Item
	Part A
	Part B

	Mixing Ratio (in weight)
	Part A : Part B = 6 : 1

	Appearance
	Milk white liquid
	Transparent liquid

	Density / (kg/L)
	1.05-1.10
	1.10-1.20

	Pot Life / h
	1-1.5

	Set-to-foot traffic time / h
	12

	Complete hardening time / days
	7

	Packing Size
	[bookmark: OLE_LINK9][bookmark: OLE_LINK8]7 kg/pail


ADVANTAGES
· High resistance to abrasion and to scratches;
· Non-yellowing;
· Dirt pick-up resistant; 
· Easy to apply; 
· Water dispersion and eco-friendly.
PROPERTIES
	Description
	Test Methods
	Typical Values 

	Abrasion resistance after 7 days (Taber abrasion meter, CS17 wheel, 1000 g, 1,000 revs)
	[bookmark: OLE_LINK13][bookmark: OLE_LINK14]EN ISO 5470-1
	≈50 mg

	Abrasion resistance after 7 days (Taber abrasion meter, CS10 wheel, 1000 g, 1,000 revs)
	EN ISO 5470-1
	≈34 mg

	Gloss (Gloss 60° C)
	ISO 2813
	10

	QUV color variation
	ASTM G 154
	more than 1,500 hours with no variation

	Permeability to water vapor
	EN ISO 7783-2
	Class I

	Capillary absorption and permeability to water
	EN 1062-3
	0.047 kg/ m²·h0.5

	Direct traction adherence
	EN 1542
	> 3.5 MPa  (rigid system with traffic)


Note: The above data were tested under standard conditions (temperature 23 °C ± 2 °C, relative humidity 50% ± 10%). 
APPLICATION INSTRUCTIONS
Application information
	Items
	Description

	Consumption
	0.1-0.2 kg/m²/coat

	Waiting time between coats (23°C)
	4 h min. / +72 h max.

	Relative air humidity
	<85%

	Substrate temperature
	[bookmark: OLE_LINK10][bookmark: OLE_LINK11]10 °C min. / +30 °C max.
≥ 3 °C above dew point, beware of condensation


*Material consumption depends on the porosity and texture of the substrate. 
Application Instructions
· Substrate preparation:
(1) For application onto newly resin-coated surfaces, the underlying resin coating must be fully cured and dry, with topcoat application carried out within 24 hours. If exceeding the 24-hour window, the resin substrate shall be thoroughly cleaned and completely free from oil, grease and all surface contaminants. Mechanically abrade the surface with a single-head floor sander fitted with 200–300 grit abrasive paper or a fine-grade abrasive pad. Upon completion of mechanical preparation, remove all dust residues by thorough vacuuming to guarantee optimal coating adhesion.
(2) For substrates of cementitious materials, apply YHFloorSeal PW only after the cementitious substrate has fully cured (minimum 24 hours, subject to layer thickness and ambient temperature). Perform light sanding beforehand, then fully vacuum away all sanding dust. In all cases, a suitable primer must be applied prior to top coating to regulate the substrate’s absorbency.
(3) For new or existing concrete surfaces, ensure the substrate is thoroughly cleaned and free from oil, grease and other contaminants prior to application. Complete thorough surface sanding, followed by industrial vacuum cleaning to eliminate all dust and ensure proper finish adhesion. In every case, apply the topcoat only after priming for effective pore sealing.
· Mixing: Mix Component A with Component B using a low-speed electric mixer until fully homogeneous, mixing only the amount that can be applied within the maximum pot life. If a non-slip finish is required, add 3–5% by weight of quartz (80-100 mesh) sand during mixing.
· Coating application: Apply 1–2 coats of YHFloorSeal PW using a short-pile roller or airless spray equipment. When applying by roller, work in two perpendicular directions. If the over-coating interval between successive coats exceeds the time recommended in the above table, lightly sand the surface of the previous coat, then thoroughly remove sanding dust by vacuum before applying the next coat. Over-coating times are shorter at high temperatures and longer at low temperatures. Ensure the area is well ventilated to facilitate drying.
TRANSPORTATION AND STORAGE
The product should be stored in ventilated areas, protected from sunlight, rain, and fire. Avoid collisions during transportation. The recommended storage temperature range is 12°C to 30°C. The shelf life is a minimum of 12 months under normal transportation and storage conditions.
[bookmark: _GoBack]PRECAUTIONS
· Do not apply YHFloorSeal PW to dusty, friable or weak substrates.
· Do not apply to wet surfaces or surfaces contaminated with oils or greases.
· Do not apply to damp substrates or those affected by rising moisture.
· Incorrect mixing ratios may prevent proper curing.
· Do not expose the mixed material to direct heat sources.
· Carbon dioxide and moisture released may impair the finish. 
· Protect the applied coating from water contact for at least 24 hours.
· When applying multiple coats, do not exceed the recommended maximum over-coating interval to ensure optimal adhesion. If exceeded, mechanically abrade the previous coat before re-coating.
· Do not dilute YHFloorSeal PW with organic solvents.
· Component B of YHFloorSeal PW may vary in shade from colorless to pale yellow. This does not affect product performance or the final finish appearance.
· The coating may discolor on contact with aggressive chemicals; however, such visual change does not necessarily indicate chemical damage. Remove any spilled aggressive chemicals immediately upon contact.
· Clean the surface using appropriate equipment and detergents suitable for the type of dirt or staining.
· Component A may exhibit a small amount of soft sediment after long-term standing, which is a normal phenomenon and will not affect product performance. Please mechanically stir Component A to uniformity before use.
HEALTH AND SAFETY
Please read the safety manual carefully, our security experts will be pleased to give you advises about safety, health and environmental issues.
DISCLAIMER
The above information and recommendations which are based on our experience are as for reference, they can't replace the customers’ own experimental results. Since our company, our representatives or distributors can't control the transportation, storage, handling and use conditions of the products, the economic disputes and the quality accident caused by improper use can't be attributed to our suggest. In any application, the customer shall be responsible to comply with obligations of third-party intellectual property rights. Without our consent, anyone shall not provide technical information to third parties.

Learn more about OYH
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